Cast vs injection overview

|  | Casting Polyurethane | Injection Moulding (TPU / Thermoplastic | Preferred process |
| --- | --- | --- | --- |
| Process overview | Hot cast poured liquids set to finished parts | Thermoplastic (pellets melted and injected under pressure, cools to solidify |  |
| Tooling | Less complex designs often open pour aluminium silicone and 3 d printed . Normally faster lead time on tools | More complex to produce and requires to work under pressure moving parts | Cast tooling is less expensive |
| Production Volume | Ideal for low volumes due to cycle times for material setting, | Ideal for volume production when repeatability is required fast cycle times , self ejecting tooling multi cavity increase throughput | Injection moulding for volumes of 50 plus |
| Part Tolerances / Precision | Lower tolerances typically 0.2mm-2.5mm depending on size of part | Much more consistent parts with tolerances 0.2mm – .254 depending on size and wall thickness | Injection Moulding |
| Design Flexibility | High — forgiving on thick walls, undercuts, large/complex shapes, and embedded inserts | More restrictive (needs draft angles, uniform wall thickness) Undercuts and increase cost of tool tenfold | Cast |
| Part Size Capability | Excellent for large, thick, or heavy parts 30kg parts are produced easily in open cast tooling | Limited by the capabilities of the machines both by weight and tie bars sizing | Cast |
| Cost Per Part | In general, due to cycle times, Cast has a higher price per unit but lower set up times , More cost effective under 10 parts | Injection moulding is a very cost-effective process due to its cycle times. However, set up times are longer | Cast low volume injection high volume |
| Green credentials | Difficult to recycle | Lower waste; thermoplastic can often be reground and reused | Injection |

### Conclusions

- Casting Polyurethane is more cost effective in lower volumes, with reduced tooling costs and set up times. Ideal for larger parts Flemthane® also excels in mechanical performance. The thermoset chemistry allows for stronger cross-linking, delivering better tear resistance, abrasion resistance, and overall toughness — ideal for harsh industrial environments where parts must withstand cuts, impacts, and repeated stress without failing.

- Injection Moulding (TPU) shines in scalability, repeatability, and cost-efficiency at higher volumes. Many projects start with casting for prototyping and validation (fast, low-cost tooling, superior material testing), then consider switching to injection moulding only if volumes justify the high tooling investment and if standard TPU properties are sufficient.

Link to injection

Link to industries   located on page to suit